Glass Firing - Sundance

Program 1: Soft tack 14:30

Program 2: Tack 14:10

Program 3: Babbles 14:60

Program 4: Fuller Fuse 14:40

To switch from one program to another.

Idle

Ramp Hold (Should see program)

Hit the desired # program (1, 2, 3, or 4)

Enter after each

Start (Twice)

Can always check review.

Glass Firing – Ann Ott

Program Created for Soft Tack Fused Glass

|  |  |  |  |
| --- | --- | --- | --- |
| RA 1 | RA 2 |  |  |
| 300 | 600 |  |  |
| F^ 1 | F^ 2 | F^ 3 | F^ 4 |
| 1220 | 1430 | 900 | 700 |
| HLD 1 | HLD 2 | HLD 3 | HLD 4 |
| .40 | .10 | .1 | .01 |

You’ll create higher temperature programs for a fuller fuse.